## Slide 1: Machinery Integrity: Synergizing Engineering solutions and AI-Driven Diagnostics
Presented by
MOHAMAD RABA’I BIN YAHAYA
PRINCIPAL ENGINEER (ROTATING EQUIPMENT)

## Slide 2
Mohamad Raba’i Bin Yahaya
rabaiyahaya@petronas.com
+(609) 831 2534
Authors Biography
Ir. Abdul Latif Bin Mohamed
alatif_mohamed@petronas.com
+(603) 2392 6109
Principal Engineer Rotating Equipment at Group Technical Solutions (GTS)
18 Years of experience with turbomachinery equipment in oil & gas industry covering operation, maintenance, troubleshooting, failure analysis and engineering design.
Graduated from Universiti Teknologi PETRONAS, Malaysia
A Custodian Engineer Rotating Equipment at Group Technical Solutions (GTS) since 2021
Specializing in Turbomachinery and has been working both upstream and downstream sectors including Petrochemical. He has vast experience in operation and maintenance, troubleshooting, failure analysis and engineering design.
A Professional Engineer registered with Board of Engineers (BEM), Malaysia and Institution of Engineers, Malaysia (IEM).

## Slide 3: The objectives of presentation are
To share the methodological approach for assessing the material integrity of power turbines, aiming to ascertain their structural robustness and operational viability
To share the utilization of digital tools in supporting the real time performance monitoring of turbomachinery

## Slide 4
Facility Background
Located at Peninsular Malaysia, the facilities are to process and transport natural gas for consumption of customers in the power generation sector as well as various industries such as petrochemicals.
Upstream
Gas Transportation
Transport processed gas
Regasification
Convert LNG
into salesgas
Gas Processing
Process PETRONAS’
upstream natural gas
Utilities
Manufacture & supply electricity, steam, industrial gases & others
Power Sector
Industries
Gas Processing & Utilities
Upstream Supply
Customers
Industries
Power Sector
Salesgas
C2, C3, C4
1
2
3
4
LNG Shippers

## Slide 5
New way of working (NWoW) require us to resolve pain points by focusing on efficient maintenance planning and failure prevention.
Notes: Pain points
In addition, we have journey for NZCE and provide the right experience as part of talent development

## Slide 6
The internal study conducted within the group indicated few pain points that contributed to Operational Expenditure (OpEx):
Major expenditure for operational expenses contributed by turbomachinery maintenance and failures.
  The maintenance interval for most of the turbomachinery equipment are still tied to OEM recommendation, especially on the major overhaul.
  High expenditure for unplanned maintenance resulted from various reliability issues
10% of the group’s overall maintenance expenditure are for unplanned Maintenance vs. best in Group of 5%
32-34% of equipment failures cost in are for GTG & GTC
Conservative Time-Based Maintenance Interval by OEM
PAIN POINTS
Source : OPEX Cost Comparison Study 2018
Notes: Pain points
In addition, we have journey for NZCE and provide the right experience as part of talent development

## Slide 7
VALUE DRIVERS
Equipment Failure prevention via effective decision making and intervention
Efficient maintenance planning to achieve competitive UPC e.g $/kWh, $/GJ
Sustain Critical equipment efficiency to support lower energy consumption & meeting GHG emission target
Provide the right experience to the staff for data analysis tools
Notes: Pain points
In addition, we have journey for NZCE and provide the right experience as part of talent development

## Slide 8
SOLUTIONING
New Way of Working (NWoW) envisioned to realize the value drivers via Engineering & Digital Solution
AI-Driven analytical tools for early anomaly detection, fault diagnostic & prescriptive, time to failure forecast
Engineering Solution
Engineering assessment to assess the integrity of critical components, enabling firm decision making to support the preventive actions and extending the lifespan of the equipment.
Digital Solution
Notes: Pain points
In addition, we have journey for NZCE and provide the right experience as part of talent development

## Slide 9: Our turbomachinery typical maintenance
There are 8 units of DR-61 Power Turbines manufactured by Dresser Rand aerodynamically coupled with gas turbine
Based on OEM Operation and Maintenance Manual, Power Turbine rotor need to be retired* at 100,000 running hours.
The challenge is to reform the mean time between overhaul for this equipment to support the plant operational excellence.

## Slide 10: DR 61 information
Package with GE LM2500 SAC Base
Heavy duty industrial design
Oil film bearings
Two-stage overhung rotor
Tip shrouded blades
Design life of 100,000 hours
Design Speed: 5,500 RPM
Maximum Continuous Speed: 5,775 RPM
Power: 31,000 HP 23,100 KW
Efficiency: 37.5%

## Slide 11: There are 2 steps to address this challenges and make it feasible
Engineering approach as part of Feasibility Assessment
Perform Remnant Life Assessment (RLA) – to access the material integrity as the Power Turbine is exposed to the thermal stress throughout the service.
Digital solution for the Sustainable Operational Performance
Using digital diagnostic tools allow us to monitor the real time performance of the equipment which enable us to monitor real time performance, perform fault diagnostic and predict the time to failure.

## Slide 12: Remnant Life Assessment (RLA) approach
Visual
Material Identification
NDT – FPI
Dimensional Measurement
Check for external defects and distortion
Optical Microscope - material structure phase, defect and grain size observation
Scanning Electron Microscope - to analyze the size, shape and distribution of particles
Hardness testing
Stress Rupture Testing – to determine the time to rupture and compared to the established TTR of the similar material
Material Testing
Microstructure
Inspection

## Slide 13: Critical component were subjected to inspection and testing
Major components (Rotating Parts) analysis
Turbine Shaft
Turbine Disc Stg 1
Turbine Disc Stg 2
Turbine Blade Stg 1
Turbine Blade Stg 2
Running Hours: ~100k & 120k
Exposure Temp: >700 DegC

## Slide 14: Shaft
Satisfactory Martensitic microstructure of Alloy Steel 4340
No significant degradation on microstructure
No evidence of significant defect & creep void
Satisfactory Hardness

## Slide 15: Disc Stage 1 & 2
Normal degradation Austenitic microstructure of Inconel 718
Material consists of fine grain structure with non-uniform size
No evidence of significant defect & creep void
Satisfactory Hardness

## Slide 16: Blade Stage 1 & 2
No crack or significant damage
No material loss due to hot corrosion
No excessive distortion or creep deflection
Satisfactory material construction (IN 738)
Satisfactory microstructures with minor degradation
Satisfactory hardness
Adequate Creep Rupture Life

## Slide 17
Stage 1 Root
Stage 2 Airfoil
Stage 1 Airfoil
Stage 2 Root
Microstructure analysis on the airfoil were found to be slightly degraded with evidence of elongated carbide precipitation formed on grain boundary. The degradation appeared to be more severe on Stage 1 Blade. No abnormal degradation such as unwanted precipitates, surface oxidation attack, creep void and micro-cracking were observed at all locations.

## Slide 18
Stage 1 Root
Stage 2 Airfoil
Stage 1 Airfoil
Stage 2 Root
SEM microstructure of Stage 1 and 2 Blade airfoil showed similar morphology, distribution and volume fraction of Gamma Prime (γ’) precipitation compared to that of blade root. However, minor coarsening of Gamma Prime (γ’) was observed in Stage 1 Blade, where the precipitates appeared to be slightly rounded in shape and measured below 2μm. No coarsening of Gamma Prime (γ’) was observed in Stage 2 Blade. The observation suggested that both Stage 1 and 2 Blades airfoil did not suffer severe material degradation

## Slide 19: Blade Stress Rupture Test
To Measure Rupture Life
Test Condition
  Temperature:845ºC
  Load: 350MPa
  Min Life: 30 Hours*
Result
  Root Stage 1: 58 hrs/ 84hrs
  Root Stage 2: 66 hrs/ 40hrs
  Airfoil Stage 1: 57 hrs/ 30hrs
  Airfoil Stage 2: 60 hrs/ 60hrs
*Based on Larson-Miller parameter graph for IN 738

## Slide 20: Remnant Life Assessment Summary
In general, all major components (Shaft, Disc and Blade) of Power Turbine were found to suffer typical operational damages with insignificant material degradation. There was no evidence of grain coarsening, creep cavity, micro-crack or other significant material defect.
The Stress Rupture Test also indicated the material time to rapture still within the expected value but reduced as compared to the test at 100k and 120k running hours.
Therefore, the MTBO extension is decided to stop at 120k hours only
Turbine Shaft
Turbine Disc Stg 1 & 2
Turbine Blade Stg 1 & 2

## Slide 21: Machinery Monitoring and Prescriptive Diagnostics (MMPD) to support operational sustenance and maintenance efficiency
The available features allow us react on time in supporting the equipment performance excellence
Early indication of anomalies
Problem cause identification and prescribe actions
Predict future values of project points based on past behavior
Prescriptive Fault Diagnostic
Predictive Trends
Forecast

## Slide 22
MMPD Features – Predictive Trending
Overall Model Residual (OMR)
Date & Time
PI Tags
Prediction trending in Green and Actual trending in Black
Deviation trending

## Slide 23
MMPD Features – Prescriptive Fault Diagnostic
Prescriptive Diagnostics with recommended actions
Faults diagnostics ranked list
Fault signature match chart
Fault Description & Possible cause
Notes: Forecast utilizing linear regression to determine whether are safe to run towards desired period.

## Slide 24
MMPD Features – Forecasting Analysis
Blue region area as the dataset
Earlier estimated TTF
Projection estimated TTF
Failure limit:
Initially pre-calculated with forecast analysis, but can be changed to follow user’s alarm setting
Level of urgency of the analysis
TTF
Earlier
Expected
Later
Projection length – is based on pre-selected historical dataset
Notes: Forecast utilizing linear regression to determine whether are safe to run towards desired period.

## Slide 25: Key takeaway from this presentation are
To have courage, is to have purpose
Purpose gives courage its direction, and courage gives purpose its potential for realization
Invoke the right tools with mastery, and the tapestry of excellence will be woven
emphasizes the importance of using the appropriate skills or resources effectively to achieve outstanding results
Adapt swiftly; thrive endlessly
by quickly adjusting to changes and challenges, one can ensure ongoing success and growth

## Slide 26
THANK YOU