Cellulose Nanocrystal-Aluminium Oxide (CNC-Al2O3) for Tribology Application in Internal Combustion Engine: Stability, Thermophysical and Tribological Behavior

Sakinah Muhamad Hisham1, 2 \*, Mohd Kamal Kamarulzaman3 \*, Norazlianie Sazali 1, 4, Kumaran Kadirgama 2, 5, 6, and Syahmi Saari 3

1Faculty of Manufacturing and Mechatronic Engineering Technology, University Malaysia Pahang Al-Sultan Abdullah, Pekan 26600, Pahang, Malaysia  
2Advanced Nano Coolant-Lubricant (ANCL) Lab, Automotive Engineering Centre, Universiti Malaysia Pahang Al-Sultan Abdullah, Pekan 26600, Pahang, Malaysia  
3Faculty of Engineering, Universiti Pertahanan Nasional Malaysia, Kem Perdana Sg. Besi, Kuala Lumpur 57000, Malaysia  
4Faculty of Mechanical and Manufacturing Engineering, Universiti Tun Hussein Onn Malaysia, Batu Pahat 86400 , Johor, Malaysia  
5Faculty of Mechanical and Automotive Engineering Technology, Universiti Malaysia Pahang Al-Sultan Abdullah, Pekan 26600, Pahang, Malaysia  
6Department of Civil Engineering, College of Engineering, Almaaqal University, Basra 61003, Iraq  
\* Corresponding author. Tel.: +6-017-652-5975; e-mail: mohd.kamal@upnm.edu.my; sakinah.hisham0704@gmail.com

Received XXX 2023, Revised XXX 2023, Accepted XXX 2023

ABSTRACT

The experimental study investigates the stability, thermophysical, and tribological characteristics of cellulose nanocrystal (CNC), aluminum oxide (Al2O3), and hybrid CNC-Al2O3 nanolubricants as additives in SAE 40 engine oil. Stability assessments were conducted through sedimentation observation, UV-visible spectroscopy, and zeta potential analysis at various concentrations (0.01% to 0.05%) and temperatures (30°C to 90°C). The hybrid CNC-Al2O3 nanolubricants demonstrated excellent dispersion stability with zeta potential values exceeding 150 mV at optimal concentrations. Thermophysical property analysis revealed that dynamic viscosity increased significantly, with the hybrid system showing a 56% enhancement at 0.03% concentration and 30°C. The coefficient of friction (COF) results showed remarkable improvement, with 0.01% CNC-Al2O3 concentration achieving a 78.6% reduction compared to base oil. The specific wear rate demonstrated progressive improvement with increasing concentration, reaching optimal values of 0.016 mm³/Nm at 0.05% concentration. These findings indicate that CNC-Al2O3 hybrid nanolubricants at optimal concentrations provide enhanced tribological performance and improved thermophysical properties, making them promising candidates for internal combustion engine applications.

**Keywords:** Hybrid nanolubricant; cellulose nanocrystal; aluminum oxide; viscosity; thermal conductivity; tribological behavior; stability analysis; wear rate; coefficient of friction; engine oil